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Fabric or leather name:
NOTE
Fabric


Description: 
Note is a soft, 100% cotton fabric with a subtle multi-colour blend that ensures a beautiful depth to any piece of furniture. The fabric has an elegant expression, adding comfort and tactility when used in upholstery.
What to know:
This textile has a distinctive, tactile character with natural shading caused by the direction of the fibres. Depending on the angle and light, the fabric may appear lighter or darker, and more matte or shiny. The change of appearance is noticeable and normal in areas where the fabric is exposed to wear and tear. The fabric develops its patina from the moment it is upholstered on a piece of furniture. Pressure marks may occur upon delivery.
Cleaning instructions: [image: asset-1.png] [image: asset-2.png] [image: asset-5.png] [image: asset-3.png] [image: asset-6.png]

Technical specifications: 
Width: 140 cm
Weight: 690 g/m
Colour fastness to light: 5-6**** - ISO 105-B02
Colour fastness to rubbing wet: Colour 1, 6, 16, 19, 20, 26 = 4-5****, colour 24 = 4****, colour 4, 9 = 3-4***, colour 14 = 3** - ISO 105-X12
Colour fastness to rubbing dry: Colour 1, 6, 16, 20, 24, 26 = 5*****, colour 4, 9, 14, 19 = 4-5**** - ISO 105-X12
Pilling: 4-5**** - ISO 12945-2
Composition: 100% cotton (CO)
Abrasion: 50.000*** Martindale - ISO 12947-2

Classification for upholstery:
poor 
** caution 
*** acceptable 
**** good 
***** very good
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