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Fabric or leather name:
PATH
Fabric


Description: 
Path is a soft, striped velour fabric that changes in the light, offering a dynamic visual language that adds something special to any piece of furniture. The blend of viscose, cotton, and polyester ensures that the fabric is as durable as it is elegant. 
Path's colour and depth changes based on the angle you view it and light in the room.
What to know:
Chenille has a distinctive, tactile character with natural shading caused by the direction of the fibres. Depending on the angle and light, the fabric may appear lighter or darker, and more matte or shiny. The change of appearance is noticeable and normal in areas where the fabric is exposed to wear and tear. The fabric develops its patina from the moment it is upholstered on a piece of furniture. Pressure marks may occur upon delivery.
Cleaning instructions: [image: asset-1.png] [image: asset-2.png] [image: asset-5.png] [image: asset-3.png] [image: asset-6.png]


Technical specifications: 
Width: 140 cm 
Weight: 920 g/rm 
Colour fastness to light: 5-6**** - EN ISO 105-B02 
Colour fastness to rubbing wet: 3-4*** - EN ISO 105-X12 
Colour fastness to rubbing dry: 4-5**** - EN ISO 105-X12 
Pilling: Grade 4-5**** - ISO 12945-2 
Composition: 45% Viscose (VI), 35% Cotton (CO), 20% Polyester (PL)
Abrasion: 30.000*** Martindale - EN ISO 12947-2 

Classification for upholstery:
poor 
** caution 
*** acceptable 
**** good 
***** very good
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