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Fabric or leather name:
PLAIN
Fabric


Description: 
Plain is a textured, pebbled fabric made from a blend of colours. Because the fabric is made from 100% polyester, it is durable and drapes easily across any type of furniture. The fabric cleans easily and retains its colour well over time, making it ideal for furniture that’s used often. 
What to know:
This is a Q2 fabric by Rohleder. This means it is designed to be durable, colour-fast, and comfortable, as well as easy to clean. The fabric is made without chemical stain-resistant finishes, so it does not have allergenic vapours. We highly recommend Q2 fabrics as family-friendly.
Cleaning instructions: [image: asset-1.png] [image: asset-2.png] [image: asset-5.png] [image: asset-3.png] [image: asset-6.png]
Technical specifications: 
Width: 144 cm

Weight: 849 g/ml

Colour fastness to light: 6**** - ISO 105-B02

Colour fastness to rubbing wet: 4**** - ISO 1205-X12

Colour fastness to rubbing dry: 4-5*** - ISO 105-X12

Pilling: Grade 3-4*** - ISO 12945-2

Composition: 100% polyester (PES)

Abrasion: 90.000**** Martindale

Classification for upholstery:
poor 
** caution 
*** acceptable 
**** good 
***** very good
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