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Fabric or leather name:
POND
Fabric


Description: 
Pond is a strong, durable woven textile made from a blend of synthetic and natural fabrics. With a soft and slightly textured hand-feel, the fabric drapes easily on any style of furniture. 
What to know:
Chenille has a distinctive, tactile character with natural shading caused by the direction of the fibres. Depending on the angle and light, the fabric may appear lighter or darker, and more matte or shiny. The change of appearance is noticeable and normal in areas where the fabric is exposed to wear and tear. The fabric develops its patina from the moment it is upholstered on a piece of furniture. Pressure marks may occur upon delivery.
Cleaning instructions: [image: asset-1.png] [image: asset-2.png] [image: asset-5.png] [image: asset-3.png] [image: asset-6.png]

Technical specifications: 
Width: 135 cm
Weight: 815 g/m
Colour fastness to light: 5-6**** - ISO 105-B02
Colour fastness to rubbing wet: Colour 14, 16 = 4****, all others colours = 4-5**** - ISO 105-X12
Colour fastness to rubbing dry: Colour 14, 16 = 4-5****, all others colours = 5***** - ISO 105-X12
Pilling: Grade 4-5**** - ISO 12945-2
Composition: 35% acrylic (PC), 23% viscose (VI), 20% polyester (PL), 12% cotton (CO), 10% linen (LI)
Abrasion: 30.000*** Martindale - ISO 12947-2

Classification for upholstery:
poor 
** caution 
*** acceptable 
**** good 
***** very good
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